##### Solution-processed doping and undoping zinc-oxide and copper-oxide thin films

# Nguyen Van Dung,1,2 Nguyen Quang Hoa,3 Tran Van Dung,2 Bui Nguyen Quoc Trinh2†*

1Vietnam National University, Vietnam Japan University, Luu Huu Phuoc street, Nam Tu Liem, Hanoi, Vietnam

2Vietnam National University, University of Engineering and Technology, Faculty of Engineering Physics and Nanotechnology, 144 Xuan Thuy, Cau Giay, Hanoi, Vietnam

3Vietnam National University, University of Science, Faculty of Physics, 334 Nguyen Trai, Thanh Xuan, Hanoi, Vietnam

†Presenter

*Corresponding author’s e-mail: trinhbnq@vnu.edu.vn

ABSTRACT

Zinc-oxide (ZnO) and copper-oxide (CuO) based thin films have attracted a huge attention owing to controllable electrical conductivity and low-cost materials for manufacturing electronic and photonic devices. In this work, we have characterized on physical properties of undoped and doped (ex.: Ag, Al) ZnO and CuO thin films, prepared by using a solution process. For formation of precursor solution, zinc/copper nitrate hexahydrate (original or doping), water and citric acid were used as metal salt, solvent and stabilizer, respectively. After that, using the precursors mixed, ZnO/CuO thin films were spin-coated on glass substrates followed by an annealing process below 550oC. Structural, morphological, optical and electrical properties of the thin films were, in turn, evaluated by using X-ray diffraction, scanning electronic microscopy, UV-vis, and four-probe measurement systems. Achievement results show that, when annealing temperatures increased from 450°C to 550°C, the thin films were oriented more preferentially along (100) (002) and (102) directions. ZnO based thin films were relatively porous, and whose band-gap energy was closed to 3.2 eV. In addition, characterization on CuO thin films will be discussed in this conference.

Keywords: ZnO, CuO, sol-gel, TFT, solar cell