The 9th International Workshop on ADVANCED MATERIALS SCIENCE AND NANOTECHNOLOGY

Ninh Binh City, Vietnam, 7-11 November 2018

Contact Address: IWAMSN 2018 Workshop Secretariat and Administration Staff

Institute of Materials Science, Vietnam Academy of Science and Technology,

18 Hoang Quoc Viet Road, Cau Giay District, Hanoi, Vietnam.

- Phone: (84-4) 3.7568870                              - Fax: (84-4) 3.8360705

- Email: iwamsn2018@ims.vast.ac.vn             - Website: http://www.iwamsn.ac.vn

## ABSTRACT FORM

(Submission Deadline: 15 August 2018)

Title:	Closed magnetic circuit magnetoelectric composites for extremely high sensitivity and electromechanical resonances controllable current sensor

Category                         Oral presentation                                       Poster presentation

Session: 	6. Advanced Metals and Composites (code: AMC)

2.  Nanostructured Materials and Devices (code: NMD)

.

Author(s):	D.T. Huong Giang, N.T. Vinh, V.T.N. Khanh, H.A. Tam, P.A. Tuan and N.H. Duc

Institution: 	University of Engineering and Technology, Vietnam National University, Hanoi

Speaker:	Do Thi Huong Giang

E-mail:	giangdth@vnu.edu.vn

Abstract:	Many assiduous researches have been taken into account by improving the increasing the soft intrinsic magnetic susceptibility of ribbon ferromagnetic phase or optimizing shape and size as well as piezoelectric/magnetostrictive volume ratio. All of these efforts lead to abate the demagnetization field. This paper describes from simulation toward experiment to find out the most effective method for enhancing magnetoelectric effect (ME) in current sensing applications. By using ring-shape magnetoelectric composites, many advantages were found includes: (i) enhance of the magnetic field concentration and (ii) eliminate impact of demagnetization field between magnetic layers thanks to closed magnetic circuit; (iii) easy to tune electromechanical resonances; and (iv) independent of the distance from the current-carrying cable. Indeed, it shows a variable resonant frequency from 20 to kHz 175 kHz depending on the size and structuce. An excellent linearly and an extremely high current sensitivity ~ 10 V/A was achieved in the Metglas/PZT/Metglas penta-layered laminates. Compared with the other close-magnetic-circuit-type current sensor topologies reported, this sensitivity is several hundred times higher. This sensor has great potential for further current sensing applications.

# Text boxes

x